Line

We have been supplying following fishing lines with quality.

Kinds of fishing line for commercial fishing or sports fishing

1. Nylon Monofilament Line
"PRAEMIUM" brand, "FORMALIS"brand

2. Super Nylon Line

3. Fluoro Carbon Line

4. Dyneema Line (Floating Line)

5. Etc

Please your  inquiry  to Vectra company

Mrs. Schein : v-trading@farlep.net

NYLON MONOFILAMENT LINE

Color : natural, green, pink, blue, gray, smoke red, clear, fluorescent

Size : 0.10mm - 4.50mm 

Being supplied in spools, or coils as regquested.

"PRAEMIUM" brand (premium grade)
typical size

| Diameter(mm) | Breaking Strength(kg) |
| --- | --- |
| 0.10 | 0.5 |
| 0.12 | 1 |
| 0.165 | 2 |
| 0.20 | 3 |
| 0.22 | 4 |
| 0.25 | 5 |
| 0.265 | 6 |
| 0.30 | 6.5 |
| 0.35 | 7 |
| 0.40 | 11 |
| 0.45 | 14 |
| 0.50 | 16 |
| 0.55 | 20 |
| 0.60 | 25 |
| 0.70 | 30 |
| 0.80 | 36 |
| 0.90 | 45 |
| 1.00 | 60 |
| 1.10 | 77 |
| 1.20 | 90 |

"FORMALIS" brand (standard grade)
typical size

| Diameter(mm) | Breaking Strength(kg) |
| --- | --- |
| 0.06 | 0.30 |
| 0.10 | 0.60 |
| 0.12 | 0.80 |
| 0.14 | 1.00 |
| 0.16 | 1.40 |
| 0.20 | 2.05 |
| 0.23 | 2.7 |
| 0.28 | 3.6 |
| 0.33 | 4.5 |
| 0.37 | 5.6 |
| 0.40 | 6.80 |
| 0.44 | 7.8 |
| 0.47 | 9.00 |
| 0.52 | 11.50 |
| 0.57 | 13.20 |
| 0.62 | 15.40 |
| 0.70 | 20.00 |
| 0.81 | 27.00 |
| 0.90 | 33.00 |
| 1..04 | 43.00 |

SUPER NYLON LINE

Better Consistent, Higher Breaking Strength, Higher Abrasion-Resistance, Better Softness, Better Casting Ability

Any color available

Any spool by length or by weight available, For example 500meter spool, 200meter spool, 50meter spool

| Diameter(mm) | Breaking Strength(kg) |
| --- | --- |
| 0.104 | 1.3 |
| 0.128 | 1.9 |
| 0.156 | 2.2 |
| 0.165 | 2.6 |
| 0.200 | 3.8 |
| 0.234 | 5.0 |
| 0.250 | 5.8 |
| 0.285 | 6.8 |
| 0.300 | 7.5 |
| 0.330 | 8.2 |
| 0.350 | 8.9 |
| 0.400 | 12.5 |
| 0.450 | 15 |
| 0.500 | 18 |
| 0.550 | 20.5 |
| 0.600 | 23.4 |
| 0.700 | 32 |
| 0.800 | 42 |
| 0.900 | 52 |
| 1.000 | 63 |

FLUORO CARBON LINE

Better limpness of line
Excellent transparency
Incomparable tensile strength and knot strength
Better abrasion resistance

Fast sinking to the targeted point
Zero water absorption rate guarantee long durability
Light refractive index almost similar to that of water, so making the line invisible in the water

Any colors available

Any spools available , for example 150meter spool, 50meter spool, 30yards, 100yards, 200yards spool

Well known sizes are as follows.
Other breaking strength available

| Diameter(mm) | Breaking Strength(kg) |
| --- | --- |
| 0.128 | 2 |
| 0.156 | 3 |
| 0.165 | 4 |
| 0.185 | 5 |
| 0.200 | 6 |
| 0.225 | 7 |
| 0.234 | 8 |
| 0.260 | 10 |
| 0.285 | 12 |
| 0.310 | 14 |
| 0.330 | 16 |
| 0.370 | 20 |
| 0.400 | 23 |
| 0.430 | 25 |
| 0.470 | 30 |
| 0.660 | 40 |
| 0.700 | 50 |
| 0.740 | 60 |
| 0.870 | 80 |

DYNEEMA LINE

Adopted Dyneema fiber by special braiding and coating

Dyneema fiber is high performance polyethylene which was developed and patterned by DSM Netherland, with strong tenacity of amazingly 3 times of Nylon(40grams/denier) and low gravity of 0.98(floating line)

Zeor water absorption and no shrinkage by heat

Dyneema has a chemical and crystalline structure which gives fhe fiber very good resistance to all kinds of aggressive agents and environmental influences

Strong resistance to UV radiation, sea water, whether and temperature cycles

Any spools available, for example 300meter spool, 100meter spool

Colors : black, grey, other colors.

Well known sizes are as follows

| Diameter(mm) | Breaking Strength(kg) |
| --- | --- |
| 0.10 | 7 |
| 0.12 | 9 |
| 0.15 | 10 |
| 0.165 | 11 |
| 0.20 | 13 |
| 0.234 | 15 |
| 0.28 | 18 |
| 0.33 | 21 |
| 0.37 | 24 |
| 0.40 | 27 |
| 0.47 | 33 |
| 0.52 | 38 |
| 0.60 | 50 |
| 0.70 | 60 |
| 0.80 | 70 |
| 0.90 | 80 |
| 1.00 | 90 |